UNITED STATES DEPARTMENT OF AGRICULTURE

NATURAL RESOURCES CONSERVATION SERVICE

#### MATERIAL SPECIFICATION

##### MS-210:  “AGGREGATE FILTERS”

210.1	SCOPE

This specification governs the quality of aggregates used for filter materials in drainage systems for subsurface field drainlines, structural drains and/or foundation drains.

210.2	QUALITY

The aggregates shall conform to the durability requirements of ASTM C-33.

210.3	GRADATION

The gradation shall conform to the requirements for the fine aggregates of ASTM

C-33, unless otherwise specified on the drawings.

Gradation for ASTM C-33 fine aggregates:

Standard Sieve Size		Percent of Material Smaller Than

3/8 inch (9.5 mm)			100

#4 (4.75 mm)			   95 to 100

#8 (2.36 mm)			   80 to 100

#16 (1.18 mm)			   50  to  85

#30 (0.60 mm)			   25  to  60

#50 (0.30 mm)			   10  to  30

#100 (0.15 mm)		     2  to  10

210.4	HANDLING

Equipment and methods shall prevent segregation of sizes or intermixing with other materials.